|  |  |
| --- | --- |
| **Project:** Warehouse refurbishment | **Project Ref:**  PRJ-123456 |
| **Client:**  Bostock Warehousing | **Client contact:**  Clive, 021 345 567 |
| **Site Address:**  45 Greensward Avenue, Christchurch | **Date on Site:**  27-May-2019 |
| **Applicator Company:**  Bob Painter | **Job Specification:**  **TG5647** |
| **Temp at start:**  25°C | **Humidity at start:**  18% |
| **Meter ref:** PSK5678 |  |

|  |
| --- |
| Ground floor |

# Film Inspections

|  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Ref:** Dry Film: 001   |  |  |  | | --- | --- | --- | | **Time:** 5:04 pm | **Location:**  Kitchen | | | Primer, Tar | **Min: 25** μm | 32 μm | | **Readings:** 25 | **Max: 39** μm | | **Readings batch:** Yg6788 | **Std Dev: 5** | |

|  |  |
| --- | --- |
| **Comments**  Nice | |
| **Remedial Actions**  Do it again | |
|  |  |

|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Ref:** Wet Film: 002   |  |  |  | | --- | --- | --- | | **Time:** 5:10 pm | **Location:**  Lounge | | | **Applicator's Name: Bob** | | **Thickness** | | **Temperature: 26** °C | | 250 μm | | **Humidity:** 19 % | | |

|  |  |
| --- | --- |
| **Comments**  Nice! | |
| **Remedial Actions**  No action required | |
|  |  |

|  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Ref:** Dry Film: 003   |  |  |  | | --- | --- | --- | | **Time:** 5:04 pm | **Location:**  Kitchen | | | Intermediate, Tar | **Min: 25** μm | 32 μm | | **Readings:** 25 | **Max: 39** μm | | **Readings batch:** Yg89788 | **Std Dev: 5** | | **Meter used:** GH678 | | | |

|  |  |
| --- | --- |
| **Comments**  Nice | |
| **Remedial Actions**  Do it again | |
| Altex Coatings Ltd |  |

|  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| **Ref:** Wet Film: 005   |  |  |  | | --- | --- | --- | | **Time:** 5:10 pm | **Location:**  Lounge | | | **Applicator's Name: Bob** | | **Thickness** | | **Temperature: 26** °C | | 250 μm | | **Humidity:** 19 % | | |

|  |  |
| --- | --- |
| **Comments**  Nice! | |
| **Remedial Actions**  No action required | |
| Altex Coatings Ltd |  |

# Additional Photos

|  |  |  |
| --- | --- | --- |
| **Figure** **1 - Wall** | |  | | --- | | **Figure** **2 - Ceiling** | |